## Slide 1
VLSI Design
COURSE CODE
Topic:
Effect of Scaling on device performance
Department of Electronics and Communication Engineering
Session - 7

## Slide 2
AIM OF THE SESSION
To familiarize students with aspects the effect of scaling on device performance.
INSTRUCTIONAL OBJECTIVES
This Session is designed to:
Discuss the effect of scaling.
Describe the effect of scaling on device performance.
LEARNING OUTCOMES
At the end of this session, you should be able to:
Discuss the effect of scaling.
Describe the effect of scaling on device performance.
Summarize the effect of scaling.

## Slide 3
Effect of Scaling/Short Channel
Gate Leakage
Carrier Velocity Saturation & Mobility Degradation.
Drain Induced Barrier Lowering
Sub-threshold Swing
Punch-through
Hot Carrier Effects

## Slide 4
Carrier Velocity Saturation & Mobility Degradation
The electron drift velocity in the channel is proportional to the electric field for lower electric field values. These drift velocities tend to saturate at high electric fields. This is called velocity saturation.
For short channel devices, the longitudinal electric field typically also increases. At such high electric fields, a velocity saturation occurs which affects I-V characteristics of the MOSFET.
Due to higher vertical electric fields, the carriers of the channel scatter of the oxide interface. This results in the degradation of carrier mobility and the reduction in drain current.
V = uE ( E is small enough)
V = Vsat ( E is strong enough)
As Vgs increases , the drain current saturates well before pinch-off occurs.

## Slide 5
Drain Induced Barrier Lowering
If the gate voltage is not sufficient to invert the surface (i.e., gate voltage < threshold voltage), the carriers in the channel will face a potential barrier that could block the flow. By increasing gate potential, we eliminate this potential barrier. But, for short channel devices, such a potential barrier is controlled by both Vgs and Vds. If this drain voltage is increased, the depletion region of the drain-body increases in size and extends under the gate. So, the potential barrier in the channel decreases leading to carriers (electrons) flowing between source and drain, even at Vgs lower than Vt. The concept of drain lowering the channel barrier and reducing the threshold voltage is called DIBL.
DIBL: drain induced barrier lowering.
DIBL = d(Vth)/d(Vds)
DIBL which refers to the reduction of threshold voltage at higher drain voltage.
The current that flows under such conditions is called sub-threshold current (off-state current).

## Slide 6: Sub-threshold Swing
Biasing a n-mos in sub-threshold region, Vgs < Vth, Vds is large enough.
Sub-threshold Swing S = d(Vgs)/d(log(Id)) = 2.3 KT/q(1+ Cd/Cox)
The smaller S is , the better it is.
Bad Sub-threshold Swing will result in higher off-state current

## Slide 7: Punch-through
When the drain bias is increased, the depletion region surrounding the drain can extend further towards the source with two depletion regions merging. This condition is called punch-through.
The punch-through effect increases with decreasing channel length. Due to punch-through, we cannot turn off the device, so the device becomes useless as shown in the figure 4.
Figure: Punch through – merging of two depletion region

## Slide 8
Hot Carrier Effects
For smaller geometric devices, the electric field increases especially near the drain. As a result, the electrons (carriers) get a significant amount of energy which are called hot carriers.
Some of them get nearly enough energy which lead to impact ionization near drain, whereby new electron-hole pairs are generated.
As an effect, it gives rise to drain-to-body current (Idb).

## Slide 9
Controlling Effects of Scaling/ Short Channel
We observed in the previous section that if channel length is small compared to the depletion regions, short channel effects become intolerable. This limits the further reduction achievable in gate length.
----------------------------
To limit these effects, the depletion region width should be reduced with corresponding reduction in channel length.
-----------------------------------------
This can be achieved by either increasing channel doping concentration or increasing gate capacitance, or both. Gate capacitance determines the gate’s control over the channel.
-----------------------

## Slide 10
Controlling Effects of Scaling/ Short Channel
Increasing Channel doping concentration
Increasing Gate capacitance, or both.
Mobility Booster: Strained Silicon Technology
Gate Leakage Reduction: High-K Dielectric
Poly Depletion Elimination: Metal Gate

## Slide 11
Problem Discussion
  Derive the relationship between Ids and Vds
  Derive the expression for transfer characteristics of CMOS Inverter.

## Slide 12
SELF-ASSESSMENT QUESTIONS
1. What is the minimum number of CMOS required for constructing a two input NOR logic gate?
1
2
3
4
Select the correct statement(s) regarding CMOS implementation of NOT gates
Noise Margin High is always equal to the noise margin low irrespective of the sizing of transistors.
Dynamic power consumption during switching is zero.
For a logical high input under steady state, the nMOSFET is in the linear regime of operation.
Mobility of electrons never influences the switching speed of the NOT gate.

## Slide 13
TERMINAL QUESTIONS
  Write about BiCMOS fabrication in a n-well process with a diagram.
  Distinguish between Bipolar and CMOS devices technologies in brief.

## Slide 14
REFERENCES FOR FURTHER LEARNING OF THE SESSION
Reference Books:
1. Sung-Mo Kong, Yusuf Leblebici, “CMOS Digital Integrated Circuits Analysis and Design” Third Edition.
2. Debaprasad Das, “CMOS DESIGN” Second Edition.

## Slide 15
THANK YOU
Team – VLSI DESIGN